## Slide 1
One Step Processing
FlexForm heated to 200º C (392º F)
(Contact heat, forced air heating, or IR/Convection Heating)
Tooling maintained at 21º C (70º F)
Cover material framed in press
Heated FlexForm transported into press
Forming pressure at 55 psi
Closed tool time varies by FlexForm material weight and type of cover material used
Cover material bonded to FlexForm without adhesives
Optional in-tool trimming
Optional in-tool bonding of secondary attachments
Optimal removal temperature for part of 35º C (95º F)
FlexForm with cover material and optional attachments stable out of tool
Parts can go directly into packaging or onto secondary operations
Average total cycle time is 55 seconds